Lec 13

P.13

Synthetic Skin Grafts - Integra

1. Integra Overview

- Integra: A bilayered dermal substitute (雙層真皮替代物) developed by Integra Life Sciences Corp. in Plainsboro, NJ.

- Primary Use: Commonly used for coverage of excised acute burns (切除急性燒傷後的覆蓋物).

2. Development Background

- Developed by Drs. Burke and Yannas at MIT during the 1980s.

- Designed for full-thickness skin defects (全厚皮膚缺損).

3. Composition

- Inner Layer (靠近傷口的一側):

- Made of a crosslinked bovine collagen matrix (交聯牛膠原基質) and chondroitin-6-sulfate (硫酸軟骨素-6).

- Acts as a dermal regeneration template (真皮再生模板), promoting neodermis (新生真皮) formation.

- Outer Layer (外層):

- Made of silicone (矽膠).

- Functions as an epidermal barrier (表皮屏障) to:

- Prevent heat and water loss.

- Block bacterial entry.

- Maintain protection until the neodermis develops enough to accept ultrathin epidermal autologous grafts (超薄自體表皮移植物).

4. Bilaminate Structure

- The bilaminate structure (雙層結構) is a common design for commercially available skin replacement devices.

- It can be used as either temporary (暫時性) or permanent (永久性) skin replacement.

P. 20

Skin Bio-Printing

1. Concept Overview

- 3D Bio-Printing (三維生物列印):

- A proof-of-concept (概念驗證) study to engineer human skin through a layer-by-layer assembly (逐層組裝) process involving fibroblasts (成纖維細胞) and keratinocytes (角質細胞).

2. Features of 3D Bio-Printing

- Precise positioning (定位) of multiple types of matrix materials (基質材料) and cells.

- Capability to construct functional tissues of various sizes with appropriate structures (結構) and cell compositions (細胞組成).

- Offers hierarchical control (分層控制), high throughput (高通量), and a tailored (可定製且具可重現性) approach.

3. Advantages

- Demonstrates the strengths of 3D bio-printing through the creation of a multi-layered, highly stratified structure (多層且高度分層的結構), making it an ideal example.

4. Skin Printing Process

- Step-by-step layer construction (逐步建構):

- Collagen layers (膠原層) printed first.

- Fibroblasts added in the next layers.

- Followed by additional collagen layers.

- Keratinocytes (角質細胞) are printed last to form the epidermis (表皮).

5. Visualization of 3D Skin

- Confocal Microscopy (共聚焦顯微鏡):

- Visualized after 7 days of culture.

- Cells are stained (染色) to show different layers:

- Epidermis: Compact, round keratinocytes (緊密且圓形的角質細胞).

- Dermis: Elongated fibroblasts (拉長的成纖維細胞).

6. Cross Section and Top View

- Layers of collagen and cells are clearly depicted in the cross-section (橫截面) and top view (頂視圖), highlighting precise 3D structuring.

P. 21

Skin Bio-Printing - Process and Visualization

1. Bio-Printing Process (Step-by-Step)

- Layer-by-Layer Construction (逐層構建):

- (i) Print the first collagen layer (第一層膠原層).

- (ii) Print the second collagen layer (第二層膠原層).

- (iii) Add a layer of FBs (fibroblasts, 成纖維細胞) or KCs (keratinocytes, 角質細胞).

- (iv) Repeat steps (i)–(iii) three times to form a multilayer base structure (重複步驟三次，形成多層結構).

- (v) Add two additional collagen layers.

- (vi) Print two layers of KCs on top to form the epidermis (表皮).

2. Top View Representation

- Dimensions:

- Collagen layers (膠原層): Entire 6 × 6 mm area.

- Cell layers (FB or KC) (細胞層): Central 4 × 4 mm area for better spatial control (更精準的細胞位置控制).

3. Key Advantages

- Precision: Multiple types of cells and matrices are accurately located in specific layers (不同細胞和基質能被精準排列).

- Scalability: High throughput process enables larger structures (高通量工藝可製作大面積結構).

- Reproducibility: Tailored, hierarchical structures ensure consistent results (層次化結構提高可重現性).

4. Final Product Visualization

- After 7 days of culture:

- Epidermis: Compact, stratified layers of KCs (緊密分層的角質細胞).

- Dermis: Fibroblasts are elongated and distributed uniformly (拉長且均勻分佈的成纖維細胞).

- Visualized using confocal microscopy (共聚焦顯微鏡).

P. 24

Laser Bio-Printing (LaBP) (Shortened)

1. Technology

- Laser-assisted BioPrinting (LaBP) (雷射輔助生物列印): Uses laser-induced forward transfer (雷射誘導向前轉移) to arrange cells in 3D structures.

2. Key Features

- Positions very small volumes (down to femtoliters, 飛升升量級).

- High resolution and cell densities (up to \(10^8\) cells/mL).

- Hydrogel precursors (水凝膠前驅物) of any viscosity can be used.

- Cells remain unharmed during printing.

3. Applications

- Mimics natural tissue by ensuring proper cell density (細胞密度) and distribution.

- Produces 3D cell models for future tissue substitutes.

4. Study Details

- Fibroblasts (murine NIH-3T3, 小鼠成纖維細胞) and keratinocytes (human HaCaT, 人類角質細胞) were printed in collagen (膠原) layer-by-layer for skin tissue.

- Generated micropatterned layers (微圖案化層).

5. Visualization

- Top: Grid structure (網格結構) of fibroblasts (green, 綠色) and keratinocytes (red, 紅色).

- Bottom: Seven alternating layers (七層交替).

- Structure: Height ~2 mm, Base: 10 × 10 mm.

- Scale bar: 500 µm.

P. 29

In Situ Bioprinting for Skin Regeneration (Shortened)

1. Type of Bioprinting Technology

- In Situ Bioprinting (原位生物列印): Printing directly at the wound site to deliver AFS cells (amniotic fluid-derived stem cells, 羊水來源幹細胞) embedded in a fibrin-collagen hydrogel (纖維蛋白-膠原水凝膠).

2. Key Features

- Uses pressure-driven, computer-controlled bioprinting device (壓力驅動且電腦控制的生物列印裝置).

- Components include thrombin (凝血酶) for gel crosslinking and fluorescent labeling (螢光標記) for cell visualization.

3. Advantages

- Promotes wound healing by evenly distributing cells directly to the wound.

- Effective for large wound repair (大傷口修復), with potential for clinical applications.

Lec 14

P. 2 Blood:

1. Functions of Blood

- Delivers nutrients (養分) and oxygen (氧氣) to cells.

- Transports metabolic waste products (代謝廢物) away from tissues.

2. Components of Blood

- Platelets (血小板):

- Initiate blood clotting (凝血作用).

- No nucleus, are fragments of cells (細胞碎片).

- Red Blood Cells (Erythrocytes, 紅血球):

- Small, disc-shaped cells (小型圓盤狀細胞).

- Primary role: Deliver oxygen to tissues (運送氧氣).

- White Blood Cells (Leukocytes, 白血球):

- Immune system cells (免疫細胞).

- Defend against foreign invaders (外來入侵者) and pathogens (病原體).

- Plasma (血漿):

- Fluid containing proteins (蛋白質), glucose (葡萄糖), mineral ions (礦物質離子), hormones (荷爾蒙), carbon dioxide (二氧化碳), and blood cells.

3. Visualization

- Top image: Blood composition in a blood vessel (血管內的血液組成).

- Bottom image: Blood flow in a tadpole tail (蝌蚪尾巴內的血液流動).

P3: Hemostasis (止血)

- Definition:

- The physiological process of stopping bleeding, involving:

1. Vasoconstriction (血管收縮): Narrows blood vessels.

2. Platelet Plug Formation (血小板栓塞形成): Platelets aggregate to form a temporary seal.

3. Coagulation (凝血): Fibrin stabilizes the platelet plug.

- The process concludes with the dissolution of the clot after tissue repair.

P4: Blood Clotting

- Coagulation (凝血):

- Blood transforms from a liquid to a gel to prevent blood loss.

- Involves:

1. Platelet activation (活化).

2. Platelet adhesion (附著) to exposed collagen.

3. Deposition and maturation of fibrin (纖維蛋白) to stabilize the clot.

Key Terms:

- Fibrinogen (纖維蛋白原): A plasma protein converted into fibrin.

- Platelet Plug (血小板栓): A temporary blockage at the injury site.

P6: Thrombosis (血栓形成)

- Definition: Formation of a blood clot (thrombus) within a vessel, which can block blood flow.

- Causes:

- Vessel wall injury.

- Stagnant blood flow.

- Hypercoagulability (高凝血性).

Complications:

1. Thrombophlebitis (血栓靜脈炎): Inflammation of veins with clots.

2. Embolization (栓塞): Movement of a clot to another location, potentially causing blockage.

P7: Catheters (導管)

- Central Venous Catheter (CVC):

- A tube inserted into large veins (neck, chest, or groin).

- Used for fluid delivery, blood sampling, or administering medications.

Materials:

- Common polymers include:

1. Silicone (矽膠).

2. Polyurethane (聚氨酯).

3. Polyethylene terephthalate (PET) (聚對苯二甲酸乙二酯).

P8-9: Blood Transfer Outside the Body

Processes:

1. Dialysis (透析):

- Removes waste and excess water from blood, mimicking kidney function.

- Types:

- Hemodialysis (血液透析): Blood is filtered outside the body using a dialyzer.

- Peritoneal dialysis (腹膜透析): Utilizes the peritoneum as a natural filter.

2. ECMO (體外膜氧合):

- Supports heart and lung functions by oxygenating blood externally.

- Types:

- VA ECMO: Oxygenated blood is returned to the arteries.

- VV ECMO: Oxygenated blood is returned to the veins.

P10: Artificial Spleen

- Purpose: Filters bacteria from the bloodstream to prevent sepsis (敗血症).

- Uses magnetic bead-based microfluidics (磁珠微流體技術) to remove pathogens like bacteria and viruses.

Sepsis Progression:

1. Early Sepsis: Immune response triggers inflammation.

2. Septic Shock (感染性休克): Severe low blood pressure leads to organ failure.

P16: Coagulation Cascade (凝血級聯反應)

- A series of chemical reactions involving clotting factors (凝血因子) and proteins.

- Result: Formation of cross-linked fibrin to stabilize clots.

- Pathways:

1. Intrinsic Pathway (內源性途徑): Triggered by blood contact with foreign surfaces.

2. Extrinsic Pathway (外源性途徑): Triggered by tissue injury.

P19: Blood Clotting with Catheters

- Problem: Catheters can trigger thrombus formation on their surfaces.

- Consequences: Blocked blood flow, infections, or embolisms.

P26: Anticoagulants (抗凝劑)

- Drugs that prevent or reduce blood clotting.

- Examples:

1. Heparin (肝素): A naturally occurring anticoagulant.

2. Warfarin (華法林): Used to prevent clots in high-risk patients.

Applications:

- Medical devices (e.g., test tubes, dialysis machines) are coated with anticoagulants to prevent clots.

P28-29: Material Requirements for Catheters

1. Biological Properties:

- Non-toxic.

- Low tendency for biofilm (生物膜) formation.

- Non-thrombogenic (低血栓傾向).

2. Physical Properties:

- High tensile strength.

- Flexible and durable.

- Radiopaque (能被X光檢測).

3. Chemical Properties:

- Stable during storage and sterilization.

- Supports surface coatings (表面塗層) like hydrogels or antibacterial agents.

P30-31: Polymers to Reduce Clotting

- Approaches:

1. Physical Modification: Adjust surface wettability (潤濕性) or texture.

2. Chemical Modification: Add hydrophilic coatings, like PEG (聚乙二醇).

3. Biological Modification: Promote endothelialization (內皮化).

P46: Blood Vessel Structure

- Artery Layers:

1. Tunica intima (內膜): Endothelium layer.

2. Tunica media (中膜): Muscle layer with elastin and collagen.

3. Tunica externa (外膜): Connective tissue for structural support.

Artery Types:

- Elastic Arteries: Near the heart; high elastin content.

- Muscular Arteries: Supply specific tissues; more smooth muscle.

P48-49: Angioplasty (血管成形術)

- Process: A balloon catheter widens narrowed arteries.

- Stent (支架): Inserted to keep vessels open.

Complications:

1. Restenosis (再狹窄): Narrowing of the artery after treatment.

2. Neointimal Hyperplasia (新內膜增生): Overgrowth of tissue inside the stent.

P50-56: Stents (支架)

- Types:

1. Bare-metal stents (金屬支架).

2. Drug-eluting stents (藥物洗脫支架): Release antiproliferative drugs.

3. Biodegradable stents (可降解支架).

Materials:

- Common: Cobalt-chromium alloy (鈷鉻合金), Nitinol (鎳鈦合金).

P64-68: Vascular Grafts (血管移植物)

- Replace or repair damaged vessels.

Synthetic Materials:

1. PET (聚酯): Non-degradable

, used for large vessels.

2. ePTFE (聚四氟乙烯): Inert, durable, reduces thrombosis risk.

Challenges:

- Achieving tissue integration and preventing thrombosis.